## Slide 1: UKOPA Databases Update September 2017

## Slide 2: Contents
Product Loss & Fault Database
Liquid Hydrocarbon Database
LUP Database
PIWG Weld Quality Database

## Slide 3: 2016 Product Loss & Fault Data
Data received from
  NG, Cadent, NGN, WWU, SGN (Southern), Ineos, Shell, BPA
Final reminders for 2016 data have been issued
  Essar, Sabic, BP, SGN (Scotland)
82 faults recorded in 2016
1 product loss incident (Other – non welded joint)
Pipeline population data updates are in progress
UKOPA Pipeline Fault Database Report will be prepared for FARWG approval by 30th November 2017

## Slide 4: 2016 Fault Data
Fault | 2016 | 2015
Ext corrosion | 52 | 49
Ext interference | 5 | 9
Girth weld defect | 0 | 2
Original construction | 1 | 12
Material (pipe defect) | 6 | 5
Dents | 0 | 21
Ground movement | 0 | 1
Other/unknown | 10 | 14
No fault | 8 | 4
Total | 82 | 117

## Slide 5: How 2016 Faults were Discovered
Method | No. | %age
ILI | 60 | 74.1
CIPS/Pearson/DCVG | 15 | 18.3
Ground Patrol | 2 | 2.5
Air Patrol | 1 | 1.2
Public | 1 | 1.2
Site Contractor | 1 | 1.2
Other/Unknown | 2 | 2.5
TOTAL | 82 | 100

## Slide 6: Fault Data
Database now contains 3788 faults
Key data:
  External corrosion – 1313
  Internal corrosion – 29
  External interference – 720
  Original construction damage – 302
  Material defect (pipe, mill damage, seam weld) – 440
  Girth weld defect - 217
  Ground movement – 40
  No fault - 47
  Other/unknown – 606
Above represents 98% of data

## Slide 7: Product Loss Data
Database contains 197 product loss incidents:
  External corrosion – 42
  Internal corrosion – 2
  External interference – 43
  Material defect (pipe, seam weld) – 16
  Weld defect - 36
  Ground movement – 7
  Unknown - 7
  Other – 44
    Towns Gas SCC – 30
    Pipe fitting welds – 4
    Leaking clamps – 3
    Lightning – 1
    Soil stress – 1
    Non welded joint – 2
    Electric cable arc strike - 1

## Slide 8: Database Developments
Operator pipeline data is becoming more complex and difficult to check and update
Pipeline data is supplied in Excel format and has been transferred to Access
Access queries are being used to extract the data required for the UKOPA product loss incidents and faults report calculations
This allows operators to supply their current data in in-house Excel format
An expenditure approval request for the additional costs of £2,500 for this development is being drafted

## Slide 9: Liquids Hydrocarbon database
Some data received
  BPA
Outstanding data required

## Slide 10: Land Use Planning Database
A database of land use planning cases has been actioned
It is proposed the database should include:
  Location and development details
  Local pipeline details and LUP inner, middle and outer zones
  Advice provided by the HSL LUP Pre-planning advice service
  Additional QRA details
  Further advice from HSE
  With FARWG approval, a request for details of recent planning enquiries will be issued to UKOPA members by the FARWG Chairman

## Slide 11: Weld Quality Database
The PIWG is completing the UKOPA Weld Quality Project which has involved:
  Inspection of pipe weld samples from operators taken from pipelines constructed in 1970s and earlier
  Confirming weld quality against i) weld standard in place at time of construction and ii) current standard (BS 4515)
  Destructive material tests on small scale samples to obtain weld material properties
The PIWG considers that the addition of weld quality records to the UKOPA database would significantly enhance the value of this project
To commence this addition to the UKOPA database, it is proposed that gas network operators provide P18 pipeline inspection records

## Slide 12: P18 Weld Quality Records
P18 Pipeline inspection reports:
  The gas networks applies the P18 procedure when working on pipelines with girth welds of unknown quality
  This procedure requires that girth welds are inspected, and if necessary repaired before any work on a pipeline is carried out
  It is proposed that the FARWG Chairman issues the following request for pipeline weld quality data to UKOPA members :
    Gas network operators – P18 weld inspection reports
    Non gas operators – weld inspection reports for operating pipelines