[image: image8.wmf]Annual Number of Reported Incidents with Product Loss

0

2

4

6

8

10

12

14

16

18

20

22

24

26

1962

1963

1964

1965

1966

1967

1968

1969

1970

1971

1972

1973

1974

1975

1976

1977

1978

1979

1980

1981

1982

1983

1984

1985

1986

1987

1988

1989

1990

1991

1992

1993

1994

1995

1996

1997

1998

Year

Number of Incidents

Incidents with product loss - fracture

Incidents with product loss - leak


1st Interim Report (Draft Form) – UKOPA FDMG
Issue Number:1

1st UKOPA Pipeline Damage Database Interim Report (Draft Form)

February 2000

Pipeline Incident Data (Leak and Rupture) and Damage Data

1st Interim Report for the Fault Database Management Group

Comprising:

BG Transco

Huntsman ICI

BP Amoco

Shell UK


Written by :
Ray Hicks, BG Technology




Alwin Fahrer, BG Technology
SUMMARY
1st UKOPA Pipeline Damage Database Interim Report
This interim report presents collaborative data from BG Transco, Shell UK and Huntsman ICI. The report is divided into two; data relating to incidents resulting in the loss of product and all incident and damage data. No predicted failure frequency data is included in this report.

Recipients of this page may obtain a copy of this report from: BG Technology, Gas Research & Technology Centre, Ashby Road, Loughborough, Leicestershire, LE11 3GR.

Telephone 01509 282525 Facsimile 01509 283131.





Contents









       Page
1
Introduction
4


1.1

Background
4


1.2

Purpose
4


1.3

Key Advantages
4

2
Description
5

3
Database Content
7
3.2 Pipeline System Data

3 Exposure

3 Transported Products

3 Product Loss Incident Data

3 Overall Incident Frequency

3 Frequency per Type of Incident

3 External Interference

3 External Interference per Diameter Class

3 External Interference per Wall Thickness Class

3 External Interference per Material Grade

3 External Interference per Area Classification

3 External Corrosion

3 External Corrosion per Wall Thickness Class

3 External Corrosion per Year of Construction

3 External Corrosion per External Coating Type

3 External Corrosion per Material Grade

3 External Corrosion per Type of Backfill

3 Detection

3 All Incident and Damage Data

3 Overall Incident Frequency

3 Frequency per Type of Incident

3 External Interference

3 External Interference per Diameter Class

3 External Interference per Wall Thickness Class

3 External Interference per Material Grade

3 External Interference per Area Classification

3 External Corrosion

3 External Corrosion per Wall Thickness Class

3 External Corrosion per Year of Construction

3 External Corrosion per External Coating Type

3 External Corrosion per Material Grade

3 External Corrosion per Type of Backfill

3 Detection

4
Discussion and Conclusions
25
1
INTRODUCTION

1.1
Background
One of the key objectives of UKOPA is to develop a comprehensive view on risk assessment and risk criteria as they affect Land Use Planning aspects adjacent to high hazard pipelines. The main multiplier in pipeline risk assessments is the per unit length failure rate which directly relates to the extent of risk zones adjacent to the pipelines. Regulators and consultants who carry out risk assessments for UK pipelines have generally relied on US and European data to provide the basis for deriving failure rates due to the shortage of verified published data relating to UK pipelines. 

With the opportunity to pool data UKOPA decided to proceed with the setting up of a UKOPA Pipeline Damage Database during May 1998. A steering group called the Fault Database Management Group (FDMG) was established to define the requirements and to direct the development of the database. This FDMG currently comprises lead representatives from four companies; BG Transco, Huntsman ICI, BP Amoco and Shell UK. 

BG Technology were selected to set-up and manage the database on behalf of UKOPA during November 1998. Development of the database was carried out during 1999 and input database ‘empty shells’ were issued to the participating companies to populate with their own pipeline and fault data. BG Technology pooled the company data into one collaborative database and this report presents the first set of incident data, from the collaborative data, for pipeline incidents resulting in the unintentional release of gas.

1.2
Purpose of the Database

The purpose of the database is to:

· be able to assign best estimate failure rates to a UK pipeline for risk assessment purposes based on UK pipeline damage data

· estimate leak and pipeline rupture frequencies to a UK pipeline, based on UK pipeline failure rate data

· provide a more realistic and rigorous approach to the design and routing of pipelines

· test design intentions to determine the effect of engineering changes (e.g.wall thickness of pipe, depth of burial, diameter, protection measures, inspection methods and frequencies, design factor, etc.)

3.2 Key Advantages

Setting up a new database allows UK pipeline operators to design the database such that it can be used in the most effective way based on their pipeline systems. The capability for the damage data to be processed using predictive models is a way of effectively extending the base data on which the various failure rates are calculated. One of the problems with creating a UK only database has been the relatively limited population of pipelines and operating experience compared to large databases such as EGIG and CONCAWE. However, by considering all types of pipeline damage, not just leaks and ruptures, and extrapolating to the probability of a leak, the extent of the database can be extended to give a more comprehensive failure frequency profile.

2
DESCRIPTION
The collaborative database has been developed as a Microsoft Visual Basic 5 32-bit executable program using Microsoft Access 97 database files for data storage. ‘Empty shell’ Input Databases have been created for each contributing company to input their own data. Two Input databases were effectively set up, one for pipelines and the other for the faults (damage and incident data) associated with that pipeline.

Users of the application can carry out functions such as the addition, modification, deletion and viewing of pipelines and faults using a series of on-screen forms. Those forms guide the user through the data in an as specified sequence.

Example screens of the two parts of the database are shown below:

1. Pipeline Input Database – Example Screen




2. Fault Input Database – Example Screen




Each company populates their input database and returns the data (.mdb file) to BG Technology who is responsible for collaborating all the data into one database. This process is intended to be carried out on an annual basis and results from the collaborative database will also be published on a regular basis.

3
Database Content

3.1

Pipeline System Data

3.1.1 Exposure

The total length of the pipeline system up to the end of 1998 for all participating companies (BG Transco, BP Amoco, Shell UK, Huntsman ICI) is 20,534 km. The exposure in the period 1954 to 1998 is 526,339 kmyrs, as illustrated in Figure 1.

[image: image1.wmf]Total Exposure

0

100,000

200,000

300,000

400,000

500,000

600,000

1954

1956

1958

1960

1962

1964

1966

1968

1970

1972

1974

1976

1978

1980

1982

1984

1986

1988

1990

1992

1994

1996

1998

Year

Exposure in  kmyr


[image: image9.wmf]Product Loss Incidents by "Cause"

0.00

0.02

0.04

0.06

0.08

0.10

0.12

0.14

0.16

0.18

External Corrosion

External Interfernce

GirthWeld Defect

Ground Movement

Internal Corrosion

Construction/material

Other/Unknown

Cause

Frequency per 1000 kmyr

1960-1998

1994-1998


3.1.2 Transported Products

The transported products include:

Natural Gas

Ethylene
 Hydrogen

Propane

Polypropylene
19,144 km

1,007 km

14 km

20 km

36 km

Gasoline

Butane

Condensate

CO

Other
7 km

20 km

24 km

36 km

226 km

3.2 
Product Loss Incident Data

A total of 236 product loss incidents were recorded over the period between 1962 and 1998. No product loss incidents were recorded prior to 1962. An annual breakdown of incidents, both leak and fracture, is illustrated in Figure 2.

[image: image10.wmf]Product Loss Incidents by "Cause"

0.00

0.02

0.04

0.06

0.08

0.10

0.12

0.14

0.16

0.18

External Corrosion

External Interfernce

GirthWeld Defect

Ground Movement

Internal Corrosion

Construction/material

Other/Unknown

Cause

Frequency per 1000 kmyr

rupture

leak


3.2.1
Overall Incident Frequency

The development of the overall incident frequency is given in Table 1.

Period
Number of incidents
Total exposure [kmyr]
Frequency

[incidents per 1000 kmyr]

1960-1993
226
422,999
0.534

1960-1998
236
525,050
0.449

Table 1

In comparison with 5 years ago the overall average failure frequency has decreased from 0.534 to 0.449 incidents per year per 1000 km pipeline. It is worth noting that EGIG data for the period of 1970 to 1997 has resulted in an average failure frequency of 0.476 incidents per year per 1000 km pipeline.

An overview of the development of this overall failure frequency over the total period of 1960 to 1998 is given in Figure 3. This figure shows the change in the incident frequency in each year being the cumulative total from 1960 onwards. In order to see the results over the last period, without influence of the past, the moving average is calculated only over the past 5 years (1960-1964, 1961-1965, 1962-1966, etc). These results are also given in Figure 3.

[image: image11.wmf]
[image: image2.wmf]Development Overall Frequency

0.00

0.20

0.40

0.60

0.80

1.00

1.20

1960

1962

1964

1966

1968

1970

1972

1974

1976

1978

1980

1982

1984

1986

1988

1990

1992

1994

1996

1998

Year

Frequency per 1000 kmyr

Overall average up to year

Moving average (past 5 years)


3.2.2
Frequency per Type of Incident
The frequency per type of incident (main causes) is given in Figure 4.

[image: image3.wmf]Overall Loss of Product Incidents Average up to Year

0.00

0.10

0.20

0.30

0.40

0.50

0.60

1960

1965

1970

1975

1980

1985

1990

1995

2000

Year

Frequency per 1000 kmyr

External Corrosion

External Interfernce

GirthWeld Defect

Ground Movement

Internal Corrosion

Construction/material

Other/Unknown


Figure 5 shows the frequency per type of incident (initiating cause) over the period 1960-1998 and the performance over only the last 5 years (1994-1998). The figures for 1994-1998 relate to that particular period.


An overview of the incident frequency by cause and type of leak in the period 1960 to 1998 is given in Figure 6.


3.2.3

External Interference
From Figure 6 it can be seen that external interference is one of the main causes for gas leakage incidents. 

3.2.3.1
External Interference per Diameter Class 

In Figure 7 the frequencies caused by  “external interference”  are given per  “diameter class”  and  “type of product loss”.


[image: image4.wmf]External Interference

Frequency per diameter class

0.00

0.02

0.04

0.06

0.08

0.10

0.12

0.14

0.16

0.18

0-4

5-10

12-16

18-22

24-28

30-34

36-42

Diameter class (inches)

Frequency per 1000 kmyr

rupture

leak




3.2.3.2
External Interference per Wall Thickness Class 

It is expected that there is a positive relationship between incidents with gas leakage caused by third party interference (outside forces on the pipeline) and the wall thickness. In Figure 8 the frequencies caused by  “external interference”  are given per  “wall thickness class”  and  “type of leak”.


3.2.3.3 External Interference per Material Grade 


3.2.3.4
External Interference per Area Classification 


3.2.4 
External Corrosion

3.2.4.1
External Corrosion per Wall Thickness Class




3.2.4.2
External Corrosion per Year of Construction

[image: image5.wmf]External Corrosion

Frequency per Year of Construction

0.00

0.05

0.10

0.15

0.20

0.25

<1963

1964-1973

1974-1983

1984-1993

1994-2003

Year of Construction

Frequency per 1000 kmyr

rupture

leak



3.2.4.3
External Corrosion per External Coating Type




3.2.4.4
External Corrosion per Material Grade




3.2.4.5
External Corrosion per Type of Backfill




3.2.5

Detection



3.3 
All Incident and Damage Data

A total of 2221 incidents were recorded over the period between 1962 and 1998. No incidents were recorded prior to 1962. An annual breakdown in incidents is illustrated in Figure 17.


[image: image6.wmf]Annual Number of Reported Incidents

0

20

40

60

80

100

120

140

160

180

200

220

1962

1964

1966

1968

1970

1972

1974

1976

1978

1980

1982

1984

1986

1988

1990

1992

1994

1996

1998

Year

Number of Incidents

Incidents with product loss - leak

Incidents with product loss - fracture

Incidents with no product loss


3.3.1
Overall Incident Frequency

The development of the overall incident frequency for all recorded incidents is given in Table 2.

Period
Number of incidents
Total exposure [kmyr]
Frequency

[incidents per 1000 kmyr]

1960-1993
2017
422,999
4.768

1960-1998
2221
525,050
4.230

Table 2

In comparison with 5 years ago the overall average incident frequency has decreased from 4.768 to 4.230 incidents per year per 1000 km pipeline.

An overview of the development of this overall failure frequency over the total period of 1960 to 1998 is given in Figure 18. This figure shows the change in the incident frequency in each year being the cumulative total from 1960 onwards. In order to see the results over the last period, without influence of the past, the moving average is calculated only over the past 5 years (1960-1964, 1961-1965, 1962-1966, etc). These results are also given in Figure 18.


[image: image7.wmf]Overall Incident Frequency

0.0

1.0

2.0

3.0

4.0

5.0

6.0

7.0

8.0

9.0

10.0

1960

1962

1964

1966

1968

1970

1972

1974

1976

1978

1980

1982

1984

1986

1988

1990

1992

1994

1996

1998

Year

Frequency per 1000 kmyr

Overall average up to year

Moving average (past 5 years)


Remainder of Section 3

Work in progress

4
Discussion and Conclusions

Work in progress

Figure � SEQ Figure \* ARABIC �1�





�LINK Excel.Chart.8 "E:\\Work\\ukopa\\Overall PIPE & Incident Exposure.xls" "G-Ann Inc PL" \a \p���





Figure 2





Figure 3





Figure 4





�LINK Excel.Chart.8 "E:\\Work\\ukopa\\Loss of Gas Incidents.xls" "G-Inc by Cause Year" \a \p���





Figure 5





�LINK Excel.Chart.8 "E:\\Work\\ukopa\\Loss of Gas Incidents.xls" "G-Inc Cause L-F" \a \p���





Figure 6





Figure 7





Figure 7





�LINK Excel.Chart.8 "E:\\Work\\ukopa\\Loss of Gas Incidents.xls" "G-EI Wall Class" \a \p���





Figure 8





�LINK Excel.Chart.8 "E:\\Work\\ukopa\\Loss of Gas Incidents.xls" "G-EI Grade Class" \a \p���





Figure 9





Figure 10





�LINK Excel.Chart.8 "E:\\Work\\ukopa\\Loss of Gas Incidents.xls" "G-EI Area" \a \p���





Figure 11





Figure 12





Figure 13





Figure 14





Figure 15





Figure 16





Figure 17





Figure 18








February 2000


UKOPA FDMG


  Page 27 of 25


_1012303942.unknown

_1012303947.unknown

_1012303950.unknown

_1012303953.unknown

_1012303945.unknown

_1012303934

_1012303936.unknown

_1012303932

_1012303929.unknown

